## Slide 1: TEM results on laser structures: AlN bulk vs. ELO-AlN as well as with/without superlattice
Anna Mogilatenko
Ferdinand-Braun-Institut Leibniz-Institut für Höchstfrequenztechnik

## Slide 2: TS4045-1: Growth on bulk AlN

## Slide 3: TS4045-1: Growth on bulk AlN
Barriers: ~ 4.5 nm
QWs: ~ 1.75-2 nm
No abrupt interfaces, symmetric QW profile

## Slide 4: TS4045-2H: Growth on ELO-AlN, no superlattice

## Slide 5: TS4045-2H: Growth on ELO-AlN, no superlattice
bottom cladding
ELO-AlN
bottom cladding
v-pits
dislocation inclination already in AlN (TU AlN/FBH AlN)

## Slide 6: TS4045-2H: Growth on ELO-AlN, no superlattice

## Slide 7: TS4045-2H: Growth on ELO-AlN, no superlattice
Al-rich layer between the bottom WG and bottom cladding
bottom cladding: used as reference Al0.8Ga0.2N
bottom AlGaN waveguide: Al0.66Ga0.34N
Interface: Al0.86Ga0.14N
Al-K
Ga-L

## Slide 8: TS4045-2H: Growth on ELO-AlN, no superlattice
Barriers: ~ 4.25-4.5 nm
QWs: ~ 1.75 - 2 nm

## Slide 9: TS4045-2H: Growth on ELO-AlN, no superlattice
profile 2
profile 1

## Slide 10: TS4045-2H: Growth on ELO-AlN, no superlattice
above a trench
step?

## Slide 11: TS4045-2H: Growth on ELO-AlN, no superlattice
above a trench
step?
profile 1
profile 2

## Slide 12: TS4048-2H: Growth on ELO-AlN with superlattice
no v-pits

## Slide 13: TS4048-2H versus TS4045-2H

## Slide 14: TS4048-2H: Growth on ELO-AlN with superlattice
superlattice
AlN
superlattice fades out
3 nm

## Slide 15: TS4048-2H: Growth on ELO-AlN with superlattice
superlattice fades out
3 nm

## Slide 16: TS4048-2H: Growth on ELO-AlN with superlattice
superlattice is there
3 nm

## Slide 17: TS4048-2H: Growth on ELO-AlN with superlattice
superlattice: 5ML x 2ML x 3ML
1.25 nm x 0.5 nm x 0.75 nm
Nominal thicknesses: 2 nm x 2 nm
bottom AlGaN waveguide
superlattice almost dissolved
Ga desorption
3 nm

## Slide 18: TS4048-2H
superlattice
superlattice

## Slide 19: TS4048-2H: Growth on ELO-AlN with superlattice
Barriers: ~ 4-4.5 nm
QWs: ~ 1.5-2 nm

## Slide 20: TS4048-2H: Growth on ELO-AlN with superlattice
QWs above a trench
4 nm

## Slide 21: TS4048-2H: Growth on ELO-AlN with superlattice
QWs above a trench
Tendency: QWs are smoother above the ridges
QWs above a ridge

## Slide 22: TS4048-2H: Growth on ELO-AlN with superlattice
QWs above a trench
profile 1
profile 2
top
QW
bottom QW

## Slide 23: Summary
QW/Barrier thicknesses are comparable
For samples on ELO-AlN slight thickness inhomogeneities above trenches
V-pits
Superlattice fades out in the middle, but is present at the beginning and at the end of the growth
ADF detector is required to show clearly the dislocation line propagation (however up to now – no noticeable changes in dislocation propagation)
Further steps for structural analysis of layers on bulk AlN? FIB-preparation?

## Slide 24: TS4045-1: growth on bulk AlN